Technical Data Sheet (TDS)

Natural Rubber Sealing Ring / NR Gasket Ring

| Product Name | Natural Rubber Sealing Ring | Product Series | JY-NR Series |
| --- | --- | --- | --- |
| Material | Natural Rubber (NR) compound | Color / Appearance | Light yellow to off-white rubber ring |
| Application | Paint/chemical can lids, clamp lids, flower-basket lids, UN lids | Issue Date | 2026-06-10 |
| Manufacturer | Jiangyin Jinyu Packaging Materials Co., Ltd. | Document Version | V1.0 |

# 1. Product Description

JY-NR natural rubber sealing rings are soft elastic gasket rings made from natural rubber compound. The product is designed for lid sealing applications where a flexible rubber ring is installed into the lid/groove and compressed during closing to provide sealing performance. Final size can be customized according to lid type, groove size and customer samples.

# 2. Key Features

Good elasticity and compression sealing performance for general-purpose can and pail lids.

Soft hardness range for easy fitting and stable closing performance.

Economical material option compared with EPDM or special solvent-resistant materials.

Suitable for manual assembly and conventional gasket-ring production processes.

One hot/adhesive joint per ring; joint strength can be checked by tensile testing.

# 3. Typical Technical Properties

| Item | Typical Value / Specification | Unit | Remarks |
| --- | --- | --- | --- |
| Hardness | 40-45 | Shore A | Representative tested value: 43 |
| Thickness | Customized, typically 4.0-6.5 | mm | According to confirmed sample/specification |
| Width | Customized, typically 8.5-9.3 | mm | According to confirmed sample/specification |
| Length | Customized, typically 890-910 | mm | According to confirmed sample/specification |
| Density | 360 ± 5 | kg/m³ | Representative internal inspection value |
| Elongation | ≥ 200; typical 205 | % | Internal tensile test record |
| Joint tensile strength | Typical 1.8 | MPa | Measured at joint area |
| Natural rubber content | Approx. 48 | % | Based on material formulation / inspection data |
| Oil content | Approx. 0.6 | % | Internal inspection data |
| Heat aging reference | Up to 115 | °C | Short-term aging reference; not continuous service guarantee |
| Joint | 1 joint per ring | pc/ring | Visual inspection |
| RoHS | Available / can be provided upon request | - | Compliance document can be arranged according to order requirement |

# 4. Chemical Resistance and Use Limitations

Natural rubber is recommended mainly for general sealing applications. It is not recommended for long-term contact with mineral oil, hydrocarbons, aromatic solvents such as toluene/xylene, halogenated solvents, strong acids or strong oxidizers. For chemical cans or special fillings, customer-side compatibility testing with actual lid, coating and filling material is required before mass production.

# 5. Recommended Quality Checks

Dimension check: thickness, width, length and ring fitting condition.

Hardness check: Shore A 40-45 unless otherwise confirmed.

Joint check: visual inspection and joint tensile test when required.

Assembly test: fit-in-groove test, closing test and leakage/sealing test with actual lid and pail/can.

Aging/compatibility test: recommended for export orders, chemical cans or long storage conditions.

# 6. Packaging, Storage and Handling

Packaging: woven bag, carton or customer-agreed packaging method.

Store in original packaging in a cool, dry and ventilated area.

Avoid direct sunlight, rain, high temperature and heavy compression during storage/transport.

Keep away from oils, aggressive solvents, strong acids, alkali and oxidizing materials.

Recommended to use by FIFO method; re-check dimensions and elasticity if stored for a long period.

# 7. Notes

The values above are typical data for reference and should not be interpreted as a final warranty of all production batches. Final product specification shall be based on confirmed sample, approved drawing and purchase order requirement. Any special food-contact, RoHS/REACH or third-party testing requirement should be confirmed before order production.

Reference documents: Internal Inspection Report No. C2026051203 dated 2026-05-12; NR Material Safety Data Sheet, Technical Specification No. 1315.